## Slide 1: formulation of suspension concentrates
dr. Péter Bohus

## Slide 2: suspensions
a disperse system in which one substance (the disperse phase) is distributed/dispersed in fine particles’ form throughout another (the continuous phase)

## Slide 3: classification of suspensions
according to the particle size of the dispersed phase
greater than 1 µm
coarse suspension
less than 1 µm
colloidal suspension
mean diameter of particles

## Slide 4: formulation of suspension
Reduction of particle size. Grinding/milling under suitable cooling
Use dispersing agents: milling aids, stabilizers against coagulation, crystal growth inhibitors
Use a thickening agent to increase viscosity of vehicle by using suspending or viscosity-increasing agents.
Use a wetting agent.

## Slide 5: special label and advice for suspension
The most important additional label for suspensions is “Shake well before use”
Stability of suspensions may be adversely affected by both extremes and variations of temperature “Store in a cool place”

## Slide 6
advantages of dispersions of solids in aqueous solutions compared to wettable powders
controlling particle size by controlling the milling conditions
incorporating high concentrations of surfactants
to enhance wetting, spreading and penetration
adding stickers
to enhance adhesion and provide slow release

## Slide 7
usually formulated using a wet milling process
wetting agent
both external and internal surfaces of the powder aggregates or agglomerates must be spontaneously wetted
dispersing agent
to break such aggregates or agglomerates into smaller units and subsequently help in the milling process
stability
any flocculation will cause a rapid increase in the viscosity of the suspension

## Slide 8: wetting of solid particles
it is necessary to wet all surfaces:
external and internal surface of aggregates and agglomerates
the purpose is to displace/replace the air entrapped between the particles of dry powder
molecules of the wetting agent should
decrease surface tension of water
diffuse quickly in solution
quickly become adsorbed

## Slide 9: wetting
Because of the high interfacial tension between solids and water; air may be trapped in these poorly wetted particles which causes them to float to the surface of the preparation and prevents them from being readily dispersed throughout the vehicle.
Wetting of the particles can be encouraged by reducing the interfacial tension between the solid and the vehicle, so that adsorbed air is displaced from solid surfaces by liquid.
Suitable wetting agents have this effect, but decrease inter-particular forces thereby affecting flocculation.

## Slide 10: components which influence wetting
Hydrophilic colloids such as acacia and tragacanth can act as wetting agents. However, care should be taken when using these agents as they can promote deflocculation.
Intermediate HLB (hydrophilic-lipophilic balance) surfactants such as polysorbates (tweens) , Sodium lauryl sulphate etc.
Solvents such as ethanol, glycerol and the glycols also facilitate wetting.

## Slide 11
The wetting tendency is larger, the smaller the contact angle or the surface tension is.
A wetting liquid is a liquid that forms a contact angle with the solid which is smaller than 90º.
A non-wetting liquid creates a contact angle between 90º and 180º with the solid.
usage
is a way to measure the wettability of a surface
shows how a liquid deposited on a solid can spread
definition
The contact angle is an angle that a liquid creates with a solid surface or capillary walls of a porous material when both materials come in contact together. This angle is determined by both properties of the solid and the liquid and the interaction and repulsion forces between liquid and solid and by the three phase interface properties (gas, liquid and solid).
contact angle and wetting
Notes: contact angle
is a way to measure the wettability of a surface
shows how a liquid deposited on a solid can spread
The contact angle is an angle that a liquid creates with a solid surface or capillary walls of a porous material when both materials come in contact together.
This angle is determined by both properties of the solid and the liquid and the interaction and repulsion forces between liquid and solid and by the three phase interface properties (gas, liquid and solid).

## Slide 12
Young’s equation
Thomas Young (1773–1829) proposed treating the contact angle of a liquid with a surface as the mechanical equilibrium of a drop resting on a plane solid surface under the restrains of three surface tensions
contact angle θ
solid/vapour (SV, SG) interfacial tension
solid/liquid (SL) interfacial tension
liquid/vapour (LV, LG) interfacial tension
L = liquid, G = gas, V = vapour, S = solid, G = V
https://www.youtube.com/watch?v=jiEKUi42r1I
Notes: contact angle
is a way to measure the wettability of a surface
shows how a liquid deposited on a solid can spread
The contact angle is an angle that a liquid creates with a solid surface or capillary walls of a porous material when both materials come in contact together.
This angle is determined by both properties of the solid and the liquid and the interaction and repulsion forces between liquid and solid and by the three phase interface properties (gas, liquid and solid).

## Slide 13
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 14
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 15: wetting agents
anionics
sulfates (lauryl sulfate: Emulson AG/LS)
sulfonates (isopropylnaphthalene sulfonate: Madeol AG/PVA)
succinates (diisooctylsulfosuccinate: Imbirol OT/NA70)
non-ionics
  ethoxylated fatty alcohols (Rolfor TR8L)

## Slide 16
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 17
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 18: antifreeze agents
glycols
glycerol
salts (ammonium sulfate)

## Slide 19
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 20
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 21: thickening agents
Thickening agents increase the viscosity of the vehicle, thereby slowing down sedimentation.
Most agents can form thixotropic gels which are semisolid on standing, but flow readily after shaking.
Thickening agents can be divided into five broad categories: natural polysaccharides, semi-synthetic polysaccharides, clays, synthetic thickners and miscellaneous compounds.

## Slide 22: thickening agents
organic or inorganic
gums and cellulose derivatives
application in gel form
activation
preservative agent
rheological properties of gel and formulated suspension

## Slide 23: synthetic thickeners
these were introduced to overcome the variable quality of natural products
  Carbomer (Carboxyvinyl polymer, Carbopol®)
  Colloidal silicon dioxide (Aerosil®, Cab-o-sil®)
  Polyvinyl alcohol (PVA)

## Slide 24: natural polysaccharides
the main problem with these agents is their natural variability between batches and microbial contamination.
xanthan gum: fermentation route
lump formation: to avoid lump formation mix with glycol or glycerol before adding to water

## Slide 25: polymeric surfactants
Emulson AG/TRN14105
Emulson AG/DSP
Emulson AG/TP1
Envi-pol 871
typically numerous anchor points → strong adsorption

## Slide 26
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 27
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 28: dispersing agents
formation of adsorption layer on the solid particles’ surface
adsorbed quantity depends onnaure os solid and adsorbing components
adsorbing components: surfactants, polymers, polymeric surfactants
viscosity/rheological behaviour

## Slide 29: dispersing agents
classification
  dissociation (anionics and non-ionics)
  traditional and polymeric (regarding structure of hydrophobic part)
  polymeric (block and comb)
expected effects
  aggregative stability, improves fluidity
  milling aid
  crystal growth inhibition

## Slide 30: dispersing agents
anionics phosphates and sulphates, sulfonates
  polyarylphenol ethoxyphosphates
    Acid Emulson AG/TRSA
    Neutralised with TEA Emulson AG/TRST, TRST60
    Neutralised with KOH Emulson AG/TRSK
  polyarylphenol ethoxysulfates:
    Emulson AG/TRSS (ammonium salt)
  other
    lignosulfonates
    certain acrylates

## Slide 31: dispersing agents
naphthalene sulfonates derivates
naphthalene sulfonate condensated with formaldehyde
  Madeol AG/OR95
  Madeol AG/W90
methylnaphthalene sulfonate condensated with formadehyde
  Madeol MW

## Slide 32: adsorption is key-event/process
adsorbed layer properties
adsorbed quantity (isotherms)
suspensibility in different hardness water at different temperatures
zeta potential

## Slide 33
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 34
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 35: antifoam agents
polydimethylsiloxanes
alcohols
fatty acids
application tricks

## Slide 36
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 37
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 38: others
pigment, colorizing agent, dye
stabilizer against degradation
buffer and pH modifier
preservative agent

## Slide 39
wetting agents
antifreeze agents
others
dispersing agents
functional agents
thickening agents
antifoam agents

## Slide 40: ingredients of suspension
active ingredients
inerts (non-actives)
functional componen and carrier (water)

## Slide 41: main technology steps to be controlled and optimized
preparation of slurry to be milled
preparation of thickening gels
milling
incorporation of thickening gel
defoaming before packaging

## Slide 42: properties to be controlled and measured (mainly CIPAC methods)
active content
density (foam content)
suspensibility
permanent foaming
pourability
wet sieve test
particle size distribution
storage stability (low and elevated temperatures, cyclic test)
compatibility
pH without and with dilution
crystal growth
viscosity (rheological profile, apparent viscosity, yield value)

## Slide 43: particle size distribution
volume/mass of particles in given size range
numbers of particles in given size range
SHAPE „distribution”

## Slide 44: the Krieger-Dougherty equation
Krieger and Dougherty proposed a semi-empirical equation for the concentration dependence of the viscosity
concentration: volume fraction

## Slide 45: polymorph crystal
solubility
grindability
crystal growth

## Slide 46: preservation of a suspension
Water is the most common source of microbial contamination.
Also the naturally occurring additives such as acacia and tragacanth may be sources of microbes and spores.
Carbosan CD 40, proxel biocides, formaldehyde, sodium benzoate.

## Slide 47: suspending agents
semi-synthetic polysaccharides
these are derived from the naturally occurring polysaccharide cellulose
  Methylcellulose (Cologel ®, Celacol®)
  Hydroxyethylcellulose (Natrosol 250®)
  Sodium carboxymethylcellulose (Carmellose sodium®)
  Microcrystalline cellulose (Avicel®)

## Slide 48: clays
these are naturally occurring inorganic materials which are mainly hydrated silicates
  bentonite
  magnesium aluminium silicate (Veegum®, Attagel ®)

## Slide 49
sedimentation, caking
stability, coagulation
wetting and foaming
crystal growth
formulation problems connected to

## Slide 50: sedimentation
settling of a lot of particles simultaneously
Stokes’ law describes of (one) spherical particle sedimentation
real system: huge particles, non spherical, system is polydisperse
properties of sedimented layer at bottom: depends on interactions of particles (attractive and repulsive forces)

## Slide 51: sedimentation
the factors affecting the rate of sedimentation are in Stokes' equation
v = velocity of sedimentation
r = radius of a spherical particle
σ = density
ρ = liquid of density
ŋ = viscosity
g = acceleration due to gravity

## Slide 52: thermodynamic instability/stability
interfacial free energy (IFE).
IFE = interfacial tension * surface area
flocculation: at secunder energy minimum (reversible changes)
aggregation: at primary energy minimum (irreversible changes)

## Slide 53: flocculation
The natural tendency of particles towards aggregation will determine the properties of a suspension. Whether or not a suspension is flocculated or deflocculated depends on the relative magnitude of repulsive/attractive forces between particles.
Deflocculated suspension: the dispersed solid particles remain separate and settle slowly. However, the sediment that eventually forms is hard to redisperse and is described as a 'cake' or clay.
Flocculated suspension: individual particles aggregate into clumps or floccules in suspension. Because these flocs are larger than individual particles, sedimentation is more rapid, but the sediment is loose and easily redispersible. Excess flocculation may prevent 'pourability' due to its effect on rheological properties.
The ideal is to use either a deflocculated system with a sufficiently high viscosity to prevent sedimentation, or controlled flocculation with a suitable combination of rate of sedimentation, type of sediment and pourability.

## Slide 54: key points
flocculated particles settle quickly and redisperse easily, whilst deflocculated particles settle slowly but tend to cake
use high performance dispersing agents
  to provide stabilization against coagulation
  to improve efficacy of milling (size reduction)
  to control crystal growth