## Slide 1: Formulációk és szurfaktánsok

## Slide 2
FORMÁLÁSI KÉMIA, FORMULÁCIÓK

## Slide 3: Formulation Chemistry:
is Mixture Chemistry
n components are in FORMULATION, the NATURE and CONCENTRATION of these components determine and influence PROPERTIES of MIXTURE
SCIENCE AND ART
EXPERIMENTAL DESIGN – MIXTURE DESIGN

## Slide 4: Trends in formulation chemistry of pesticides

## Slide 6: HAZARD COMPONENTS TO BE REPLACED or LIMITATION OF THEIR APPLICATION
Nonylphenol derivatives
N-methyl pyrrolidone
Keton solvents (cyclohexanon, isoforone)
Aromatic C9 solvents: use naphthalene depleted versions
High volatile and/or low flash point solvents
Rhodamin B colorant
Tallow amine ethoxylates (request of substitution due to fish toxicity)

## Slide 7: Systems containing “nanoparticles” NANOTECHNOLOGY
Solubilised lipophilic active ingredient in aqueous phase
Microemulsions
Nanosuspensions (nucleation technology route)
Molecular capsulation (cyclodextrin as carrier)
Nanocapsulations (Liposomes)
Challenges: Preparation and Stabilisation
Efficacy and Phytotoxicity (adjuvancy : effect of nano-size)

## Slide 8
Formálás célja: a szükséges hatóanyag mennyiséget egyenletesen eloszlatva célba jutassuk valamilyen alkalmazási módszerrel
Célterület: talaj, levél, mag,(postharvest: gyümölcs)
Alkalmazás i módszer: folyadék, por vagy granulátum kijuttatása
Hatóanyag tulajdonságai
Forma-tipus

## Slide 9
Folyadék kijuttatás
permetezés
Porlasztás nedves csávázás (seed treatment, seed coating)
Ködképzés,aeroszol

## Slide 10: osztályozás
Higitandó vagy használatra kész (ready to use )termék
Megjelenés: egyfázisból vagy több fázisból álló készítmény
Halmazállapot: szilárd vagy folyékony készítmény
Hatóanyagok száma szerint: straight (egy hatóanyag) vagy kombináció
Hatóanyagfelszabadulás (release): slow release,controlled release, immediate/conventional release
Tartalmaz hatásfokozót (adjuváns) vagy nem tartalmaz

## Slide 11
Folyékony készitmlnyek
két diszpergált fázist tartalmazók
Egy diszpergált fázist tartalmazók
Oldatok és nano-rendszerek
SL,EC,DC,ME,MEC
SC,OD,FS,CS,EW,EO
SE,ZC
MEGJELENÉS: FÁZISOK SZÁMA SZERINT

## Slide 12
Permetlé készitéséhez alkalmas szerformák
Szilárd készitmények
SG,WG (WDG,DF)
WP
Folyékony készitmények
Oldatok, diszperziók

## Slide 13: Mixture chemistry
Hatóanyagot inert komponensekkel összekeverve kémiailag és fizikailag stabil terméket állítunk elő
Ha n számú komponens van a termékben, akkor xi szumma= 1 ahol xi az i-dik komponens tömegtörtje (koncentrációja)

## Slide 14
Legfontosabb „inert „ komponens: SURFACTANT

## Slide 15
Egyszerűen – képekkel/ábrákkal - a tenzidekről

## Slide 16: Surfactant
Surface active agent (tenzid): adszorbeálódik határfelületen
Micellákat (asszociátikumokat)képez
Amfifil szerkezete van: hidrofil és hidrofób szegmensre osztható fel a molekulák

## Slide 17
Sematikus ábrázolás

## Slide 18
Orientáció határfelületen

## Slide 19
Egy lehetséges micella: gömbalak

## Slide 20
Tenzid vizes oldata

## Slide 21: Surfactant Aggregates
4 nm
Unimers
Normal micelles
spherical
cylindrical
Bilayer lamella
Reverse micelles
Inverted hexagonal phase
Notes: Molecules of amphiphilic surfactants in solution self-assemble into various supramolecular aggregates. This slide shows typical changes in surfactant self-assembly and morphologies formed with decreasing water content in the system (water content decrease is shown by arrows)

## Slide 22
0
2
4
6
8
10
12
14
0
1
Surfactant concentration
CMC

Critical Micelle Concentration
CMC
Below CMC only unimers are present
Above CMC there are micelles in equilibrium with unimers
Notes: Critical micelle concentration (CMC) can be determined by surface tension measurements. Below CMC surfactant adsorbs on the surface and decreases surface tension. More surfactant we have below CMC less surface tension is. Above CMC the micelles are formed. All surfactant added in excess of the CMC incorporate in the micelles. Therefore surface tensions remains the same as at CMC.

## Slide 23
Solution Properties
0
2
4
6
8
10
12
14
0
1
Surfactant concentration
CMC
Concentration
unimers
micelles
0
2
4
6
8
10
12
14
0
1
Surfactant concentration
CMC
Osmotic pressure

0
2
4
6
8
10
12
14
0
1
Surfactant concentration
CMC
Isc
Light scattering
Notes: Dependencies of various solution properties on surfactant concentration reveal a break upon crossing the CMC as a result of micelle formation. This underlies methods for determining CMC by measuring such properties as a function of the surfactant concentration.

## Slide 24: Solubilization
Spontaneous transfer of a compound insoluble in the bulk solvent into solution due to incorporation into the surfactant micelles
polar compound
Reverse micelles
non-polar compound
Normal micelles
amphiphilic compound

## Slide 25: Solubility Effects
Solubility of a poorly soluble compound increases as a result of solubilization in the micelles
0
2
4
6
8
10
12
14
0
1
Surfactant concentration
CMC
Solubility
Notes: One method to characterize CMC of a surfactant in aqueous solution is to determine solubility of a water-insoluble dye as a function of surfactant concentration. Above CMC the dye is transferred into solution due to incorporation into the core of the micelles.

## Slide 26
no wetting
incomplete wetting
complete wetting
= 0°
< 90°
= 90°
> 90°
= 180°
Ө
Ө
Ө
Ө
Ө
γ s– γsL< 0
γ s – γsL ≈ 0
γ s – γsL> 0

## Slide 27: Nedvesedés, kapilaritás

## Slide 28: CMC befolyásolása

## Slide 29: A tenzid szerkezete hogyan befolyásolja a CMC-t

## Slide 30
Összesités tenzidekről bonyolultabban

## Slide 31: osztályozás
Természetben előforduló vagy szintetizált
Polimer (makromolekula)felépitésű vagy nem (adszorpciós viselkedés)
Funkció szerint: nedvesitőszer, diszpergálószer, emulgátor, szolubilizáló
Alkalmazási cél szerint: funkcionális hatás közvetlen érvényesitése és/vagy hatásfokozás (a biologiai hatás elősegitése)
Hidrofób csoport vázában a szénatomon kívül milyen atomok szerepelnek
Hidrofil csoport,szegmens mit csinál vizben: disszociál vagy nem disszociál ionokra

## Slide 32: Hidrofób csoport váza
C és H atomok
C,H és N atomok
C és F atomok (H atomok helyett)
Si atomot tartalmazó hidrófób váz

## Slide 33: Hidrofil csoport szolvatálódása vizben
  1) nem disszociál: nem-ionos (non-ionic)
  2)disszociál: ionos: disszociációt követően a hidrofób részhez kapcsolodó hidrofil csoport negativ töltésű vagy pozitiv töltésű vagy esetleg negativ és pozitiv részre tagolodik
  3) extended: tartalmaz nem disszociálódó és disszociálódó hidrofil csoportot(csoportokat ) egyaránt

## Slide 34: Ionos surfactant
Anionosak (anionic)
Kationosak (cationic)
Amfoter (amphoteric, zwitterionic)

## Slide 37: Classification of Surfactants
Anionic
Cationic
Zwitterionic
Nonionic
Sodium dodecylsulfonate
Cetylpyridinium bromide
Dipalmitoylphosphatidylcholine (lecithin)
Polyoxyethylene(4) lauryl ether (Brij 30)
Notes: You will find many other examples of amphiphilic surfactants in the recommended literature

## Slide 38: Példa az amfoter tenzidre: adjuváns glyphosate IPA oldatokhoz alkyl betaine
Cocoamidopropyl betaine

## Slide 39
Anionos felületaktivak

## Slide 40: Anionos tenzidek
Karboxilátok, sarcosinátok , ethoxycarboxylates
Szulfátok, ethoxysulfates
Szulfonátok
Foszfátok, ethoxyfosfates
Szulfoszuccinátok
Taurátok
isothionátok

## Slide 41: Karboxilátok
zsirsavakból készitett szappanok , az alkáli-sók jól oldódnak vizben
A kalcium és magnézium sók rosszul oldódnak vizben (magas keménységű vizekben kicsapodás tapasztalható
Citromsavas származékok extended tipusként alkalmazást nyernek (nedvesitőszerek)

## Slide 42: Sulfates, ethersulfates
Laurylsulfate sodium salt: wetting agent, WP,WG, esetleg SC,hátránya: erősen habzik Emulson AG/LS
Lauryl ether sulfate sodium (EO 2 vagy 3): weetingagent, built-in adjuváns glyfosinate SL-hez
Tristyrylphenol ethoxylate sulfate (extended): Emulson AG/TRSS (ammonium só: sulfamic savval készül), pH erősen savas

## Slide 43: Sulfonates
C-S kötés
Hidrofób váz: aromatic ring-t tartalmazó
  Lignosulfonates: diszpergálószerek (WP,WG)
  Naftalinsulfonates: wetting agent Madeol AG/PWA
  Naftalin illetve alkylnaphthalene sulfonates condensated with formaldehyde (Madeol AG/OR95, Madeol AG/WA90, Madeol MW
  Alkylbenzene sulfonic acid and salts: sodium salt wetting agent, calcium salt emulsifier, aminsó: emulsifier
    Alkyl csoport lauryl, dodecyl, tetrapropylene lánc
    Linerási biodegrábilisabb mint az elágazó
    Különbözó oldószerek: n-butanol, i-butanol, n-octanol, i-octanol

## Slide 44: Egyéb szulfonátok
Olefin-sulfonates: nedvesitőszerek

## Slide 45: Foszfátok (foszfátészterek)
Extended foszfátok
  Nonilfenol etoxilátumból készülő foszfátok
  Tistirilfenol etoxilátumból készülő foszfátok
    Emulgátor Emulson AG/TRSA (savforma)
    Diszpergálószer Emulson AG/TRST (TEA só), Emulson AG/TRSK (K só)
  Alkohol etoxilátumból készülő foszfátok:
    Emulgátorok Rolfen 12/13/300 (emulgátor ásványi olaj emulgálásához)
    Kompatibilitás fokozók, diszpergálószerek

## Slide 46: Foszfátok kémiája
Foszforsavval vagy fosforpentoxiddal történő észterezés
A foszfatáló komponens mennyisége változtatásával a mono-,di- és trifoszfát aránya változik a végtermékben
A trifoszfát nem-ionos tenzid, a mono- és di-foszfát anionos tenzid

## Slide 47
Nem-ionos felületaktivak kémiája

## Slide 48: Nem-ionos felületaktivanyagok
Alkoxy csoportot nem tartalmazó észterek: cukormolekula észterkötésben
Alkyl polyglucosides (APG) :glükóz származékok, éterkötésben a cukormolekula
Polyglycerol termékek
Alkoxilátumok (etoxilátumok, propoxilátumok stb.)

## Slide 49: Etilénoxid, oxirán
Etoxilálási fok: átlagos etoxilálás mértéke, különböző nagyságú molekulák >> azonos CAS szám
Növekvő etoxilálási fok >növekszik a vizoldhatóság, növekszik a CLOUD point
HLB

## Slide 50: Propilénoxid, oxirán-metil
Hidrofóbitást növeli
EO/PO kondenzátumok:
block-polimerek
poloxamerek
random polimerek (micellaképződés „fékezett”)
EO/PO kondenzátumok: Emulson AG/104, Emulson AG/105, Chimipal PE 403, Emulson AG/TRS204, Emulson AG/TRS204N

## Slide 51: D-sorbitol (C6H14O6)

## Slide 54: polymeric surfactants

## Slide 55: Definitions
Amphiphatic molecule characterised by repetitive, identical monomeric units
Molecular weight MW >1000 g/mole
Solution shows interfacial surface tension changes, surface potential modifications, interfacial phase rheology

## Slide 56: Traditional surfactants and Polymeric surfactants
Main difference with monomeric surfactants (traditional):
slower micellisation
stronger interfacial adsorption
Hence are excellent stabilisers

## Slide 57: Types of Synthetic Polymeric Substances
Homopolymers
Copolymers
A-B block copolymers
A-B-A block copolymers
(BAn) graft copolymers
Random copolymers

## Slide 58: Structural Units In Surfactant Molecules
Hydrophil/Hydrophobe or Lipophobe/Lipophil parts
Anchoring chain and Solubilising Chain built from monomeric units
Charged and Uncharged Molecules (ionic and non-ionic molecules)

## Slide 59: Polymeric Structure >> Repetitive Units in anchoring chain
Multiple anchoring points at interface
Strong steric and/or electrostatic barrier against coalescence (in emulsion) or coagulation (in suspension)
Better or fully coverage on surface represents more irreversible adsorption layers

## Slide 60: Properties of Adsorption Layers of Polymers
At lower concentration : flat-on adsorption ; adsorption layers have high concentration and low thickness
At higher concentration: tails-trains-loops adsorption; adsorption layer becomes thicker and less concentrated
Increase in interfacial viscosity

## Slide 61: Some Functions of Polymeric Substance in Formulations (1)
In Liquid Fomulations (SC, SE, EW)
  Dispersing agent/emulsifier
  Crystal growth inhibitor
  Thickening agent
  In order to improve suspensibility or emulsion stability, to improve storage stability, to prevent sedimentation/ separation, to avoid the formation of dilatant sediment

## Slide 62: Some Functions of Polymeric Substance in Formulations (2)
In Solid Formulations (WG,WP)
  Dispersing agent
  Binder, agglomeration agent
For Solid Formulations (WG,WP)
  Dispersing agent
  Binder, agglomeration agent
  Water Soluble Bags

## Slide 63: Other Applications
Seed Treatment Formulations
  filming, coating agent
Anti-Drift Properties for Sprayable Formulations
Rainfastness
Compatibility agent

## Slide 64: Natural and Synthetic Products
Natural polymers based on polysaccharides
Polyelectrolytes based on lignins
Polyelectrolytes based on naphthalene sulfonates (or alkylnaphthalene sulfonates)
Fully Synthetic Polymers

## Slide 65: Typically low condensation degree products
Naphthalene derivates
Methylnaphthalene derivates
Cresol derivates
Condensation degree: 2-10
Sulfonation degree is similar to condensation degree, condensation with formaldehyde, products always contain sodium sulfate

## Slide 66: Other polyelectrolytes
having aromatic rings
  Lignin sulfonates (sodium, calcium or ammonium salts)
  Modified lignin sulfonates
without aromatic rings
  acrylates
  modified acrylates

## Slide 67: Anchoring groups, points for hydrophobe interactions
Groups containing delocalised electrons (conjugated double bounds..)
  aromatic rings
Groups no containing delocalised electrons

## Slide 68: A-B-A block polymeric compounds
Atlox 4912 is 12-Hydroxystearic acid, polyethylene glycol copolymer (CAS Reg. No. 70142-34-6), with a minimum number average molecular weight (in amu) 5,000. This product is EPA
approved ( 40 CFR 180.1001 (c) and (e) )

## Slide 69: SORBITAN: (3S)-2-(1,2-Dihydroxyethyl)tetrahydrofuran-3,4-diol